Elemental Compositions of Herodian Prutah, Copper Coins – of the Biblical “Widow’s Mites” Series -- via Energy Dispersive X-Ray Fluorescence

Meghann Mouyianis,1 Jeffe Boats, 2 and Mark A. Benvenuto1*

(1) Department of Chemistry & Biochemistry, University of Detroit Mercy, 4001 W. McNichols Rd., Detroit, MI 48221, (2) ) Department of Mathematics and Computer Science, University of Detroit Mercy, 4001 W. McNichols Rd., Detroit, MI 48221

Abstract

Thirty six small, copper coins issued under the authority of Herod Agrippa I were analyzed using energy dispersive X-ray fluorescence spectrometry for copper, zinc, tin, lead, antimony, iron, gold, silver, and several other elements. This series of coins appears to show additions of lead to each coin, but an otherwise unadulterated bronze composition.  The metallurgical make up of the samples and implications of the findings are presented here.

Introduction

The coins of the Herodian Kings, as well as coinage of other subordinate kings and rulers of the Roman Empire, were tolerated in the early imperium, producing an overall coinage system that was Roman throughout the Empire, but that had areas of local production and influence as well.  The coins analysed in this study, the prutah, each display what appears to be three wheat ears on one side, and an umbrella on the other (1).  These or their smaller siblings are often referred to as “widow’s mites” because of the Biblical reference to them.  According to the King James Bible, Mk 12: 41-44:

“And Jesus sat over against the treasury, and beheld how the people cast money into the treasury; and many that were rich cast in much.

And there came a certain poor widow, and she threw in two mites, which make a farthing.

And he called unto him his disciples, and saith unto them, Verily I say unto you, That this poor widow hath cast more in, than all they which have cast into the treasury;

For all they did cast in of their abundance; but she of her want did cast in all that she had, even all her living.”

It is difficult today to determine what value such coins had in ancient times, but it is certainly apparent that these were the small change of their era and locale.  Whether Herodian coins were used in other transactions besides those involving the Temple treasury is also difficult to determine exactly.  But it seems logical to conclude that there was most likely other local, commercial uses for such coinage as well.

Older references to these coins simply indicate them to be copper or brass (1,2).  The experiences of our research and that of others indicates that ancient alloys are usually more complex than either a single element, or a simple alloyed mixture (3-12).

Experimental Conditions

The spectrometer used was a Spectrace QuanX energy dispersive X-ray fluorescence instrument, utilizing a rhodium target X-ray tube, fundamental parameters software, and pure element standards.  Sample excitation conditions were: 30kV, 0.10mA, 100 sec count, K for Fe, Co, Ni, Cu, Zn, As, Pt, Au, Bi, and Pb, followed by: 50kV, 0.72mA, 60 sec count, for Pd, Ag, Sn, and Sb.  Certified brass samples were run each day prior to sample runs to ensure instrument accuracy and precision.  Samples underwent sonication in hot, soapy water for 15 minutes, to ensure surfaces were clean and free of any surface contamination.

Discussion

Coins and artifacts of the Roman Empire have been studied extensively, (4,5,13-33) but these small, copper coins of King Herod seem to have been omitted from all previous examinations.  The iconography of the coins in this sample set is crude, but all have at least a recognizable wheat ear side or umbrella side.  A worn state or weak design elements are actually not detractors in this case.  Rather, one can argue that because of the wear the surfaces being analyzed do not suffer from any elemental enrichment process at a surface that might have resulted from the original method of manufacture.

This set of coins was analyzed twice on each side as a minimum, and the results averaged.  They appear to be essentially a ternary alloy: copper, tin, and lead.  Figure 1 displays the copper percentages of the samples in comparison to each other.  While the samples with the lowest percentages are near 70%, nearly half of the sample set shows 90% or higher copper.  Samples of ancient coinage with this level of purity are not unheard of (4), butare not common.

Figure 2 illustrates the lead percentage of each coin in the study, again, in comparison to each other.  Note that the y-axis peaks at 30%, thus emphasizing the lead differences somewhat in relation to the copper.  Coins WM4, WM18, and WM30 are all high in lead, and predictably, are also low in copper.  It is noteworthy however, that over half of the samples contain less than 10% lead.  This is much lower than in other studies of ancient or medieval coinage (5, 11, 34, 35).

Figure 3 shows the percentages of tin in each sample, compared against each other, in similar format to Figures 1 and 2.   In this case, the y-axis peaks at 20%, because the samples contain a relatively small amount of tin in relation to copper.

It is immediately evident that there is less tin as an average for the coins than there is lead – the mean lead percentage is 9.9%, compared with only 7.3% tin.  Also noteworthy is the relatively large sample standard deviation of 6.8% in lead percentage, compared with its mean of 9.9%, indicating a wider variation in lead content.

Beyond this, iron is present in the range of only 0.2% - 0.8%, which is both quite low and rather uniform.  Other studies of coins from different cultures and times show similar, low iron percentages (4, 5, 11, 34), and there appears to be disagreement among scholars as to whether iron in the alloys was present in original ores, is a purposeful addition to the alloy, or is a by-product of the alloy being molten in an iron container (36).  In the case of these 36 coins it remains noteworthy that so little iron was found in any of the samples.

Other elements for which this sample set was analyzed were in statistically insignificant amounts.  Silver, and gold, which are present in numerous copper ores even today (and the recovery of which sometimes pays for the electcrical requirements of copper refining) are notably absent from these coins.  In addition, only trace amounts of zinc appear, and in less than one quarter of the coins.

Conclusions

The coins are leaded bronze.  The almost complete absence of zinc indicates they are definitely not brass.

The elemental composition shows surprisingly clean make ups overall, considering the technological abilities of the age and culture.  This could be an indicator that the ancient Judaean foundry workers and minters had access to remarkably pure ore sources, or could be evidence of their ability to refine those less pure ores which were available to them.

The presence of lead in this series of coins appears to be an indicator that the mint workers had some knowledge of leaded alloys and their metallurgy, specifically the knowledge that an alloy was easier to work upon the addition of lead (because the resultant alloy had a lower melting point).

Another possibility, that lead in roughly the same percentage or ratio simply happened to be present in original copper or tin ores, seems less likely, because of the variation in lead content from coin to coin.

References

- Reinach, T.  Jewish Coins, Argonaut, Inc. Publishers, Chicago, 1966.

- Sayles, W.G.  Ancient Coin Collecting VI, Krause Publications, Iola, WI, pp.111-2, 1999.

- J. Lutz and E. Pernicka, ‘Energy dispersive X-ray fluorescence analysis of ancient copper alloys: empirical values for precision and accuracy’, Archaeometry, 38 (1996), pp.313-323.

- Irice Ellis and Mark Benvenuto.  Chemical Composition of Minor, Copper-Based Coins of the Byzantine Empire via Energy Dispersive X-Ray Fluorescence Spectrometry. Journal of Undergraduate Chemistry Research, 4, 107-112, (2005).

- G.F. Carter, ‘The chronology of Augustan asses and quadrantes determined from chemical compositions’, American Journal of Numismatics, 7-8, (1997), pp. 235-250.

- C.W. Beck, ed., Archaeological Chemistry (American Chemical Society, Washington, DC,1974), pp. 22-33, 124-147.

- G.F. Carter, ed., Archaeological Chemistry II, (American Chemical Society, Washington, DC, 1978), pp. 347-379.

- J.B. Lambert, ed., Archaeological Chemistry III, (American Chemical Society, Washington DC, 1984), pp. 273-332.

- R.O. Allen, ed., Archaeological Chemistry IV, (American Chemical Scoiety, Washington, DC, 1989), pp. 159-232.

- M.V. Orna, ed., Archaeological Chemistry: Organic, Inorganic, and Biochemical Analysis, (American Chemical Society, Washington, DC, 1996), pp. 64-82, 83-93, 94-106

- K.A. Jakes, ed., Archaeological Chemistry: Materials, Methods, and Meaning, (American Chemical Society, Washington, DC, 2002), pp.231-246.

- H. Mabuchi, K. Notsu, S. Nishimatsu, K. Fuwa, H. Iyama, and T. Tominaga, ‘[Chemical composition of ancient coins]’, Nippon Kagaku Kaishi, 5 (1979), pp. 586-90.

- G.F. Carter, ‘Zinc Content of Neronian Semisses and Quadrantes and the Relative Value of Zinc and Copper in the Coins of Nero,’ The American Numismatic Society Museum Notes, 33, (1988), pp. 91-106.

- J.A Sheridan, ‘The Nome Coins of Alexandria, Another Look,” The American Numismatic Society Museum Notes, 33, (1988), pp. 107-110.

- J. Long, ‘A New Solidus of Julian Caesar,’ The American Numismatic Society Museum Notes, 33, (1988), pp. 111-118.

- M. Paz Garcia-Bellido, ‘Punic Iconography on the Roman Denarii of M. Plaetorius Cestianus,’ The American Journal of Numismatics, 1, (1989), pp. 37-50.

- W.E. Metcalf, ‘Rome and Lugdunum Again,’ The American Journal of Numismatics, 1, (1989), pp. 51-70.

- F.S. Kleiner, ‘Galba and the Sullan Capitolium,’ The American Journal of Numismatics, 1, (1989), pp. 71-8.

- M.E. Hoskins Walbank, ‘Marsyas at Corinth,’ The American Journal of Numismatics, 1, (1989), pp. 79-88.

- E. Haley, ‘The Roman Bronze Coinage in Britain and Monetary History from A.D. 293 to 350,’ The American Journal of Numismatics, 1, (1989), pp.89-116.

- R. Newman, ‘A Dialogue of Power in the Coinage of Antony and Octavian (44-30 BC),’ The American Journal of Numismatics, 2, (1990), pp. 37-64.

- C.P. Jones, ‘Heracles at Smyrna,’ The American Journal of Numismatics, 2, (1990), pp.65-76.

- B.L. Damsky, ‘The Stadium Aureus of Septimus Severus,’ The American Journal of Numismatics, 2, (1990),  pp. 77-106.

- J. Ermatinger, ‘The Circulation Pattern of Diocletian’s Nummus, ’ The American Journal of Numismatics, 2, (1990), pp. 107-118.

- S. Cerutti, ‘Brutus, Cyprus, and the Coinage of 55 BC,’ The American Journal of Numismatics, 5-6 (1993-94), pp. 69-88.

- P. Kos, ‘Festive Issues of Galerius from the Tetrarchic Mint of Siscia,’ The American Journal of Numismatics, 5-6 (1993-94), pp. 89-96.

- R.G. McAlee, ‘Vespasian’s Syrian Provincial Coinage,’ The American Journal of Numismatics, 7-8 (1995-96), pp. 113-144.

- W.E. Metcalf and W.J. Fulco, S.J., ‘Coins from the Excavations at Tell Nimrin,’ The American Journal of Numismatics, 7-8 (1995-96), pp. 145-54.

- K. Butcher and M. Ponting, ‘A Study of the Chemical Composition of Roman Silver Coinage, A.D. 196-97,’ The American Journal of Numismatics, 9, (1997), pp. 17-36.

- J.M. Galst, ‘A New Variety of a Roman Provincial Tetradrachm from Neapolis,’ The American Journal of Numismatics, 10, (1998), pp. 103-4.

- M. Beckmann, ‘The early gold coinage of Tajan’s sixth consulship,’ The American Journal of Numismatics, 12, (2000), pp. 119-56.

- F.S. Naiden, ‘Supplication on Roman Coins,’ The American Journal of Numismatics, 15, (2003), pp. 41-52.

- W.C. Holt, ‘The Evidence of the Coinage of Poemenius’ Revolt at Trier,’ The American Journal of Numismatics, 15, (2003), pp.61-76.

- T. Gaines, E. McGrath, R. Langrill and M. Benvenuto, 'Chemical Compositions of Some of the Japanese Kanei-Tsuho Coins via Energy Dispersive X-Ray Fluorescence,' Numismatic Chronicle, 161, (2001), pp.308-317.

- D. Hartill, 'A Study of the Metropolitan Coinage of Qian Long,' Numismatic Chronicle, 151, (1991), pp. 67-120.

- Personal communication between M.A. Benvenuto and G. Travis, Numismatic Consultant, NC.

Figure Captions

Figure 1:  Copper Percentages

Figure 2:  Lead Percentages

Figure 3:  Tin Percentages

Figures

Figure 1:  Copper Percentages

Figure 2:  Lead Percentages

Figure 3:  Tin Percentages